## Slide 1: Quantifying Cement Systems using Image Analysis
Colin Leung
Cement Chemistry Team
December 13th, 2011

## Slide 2: Contents
Introduction
Purpose of Investigation
Sample Information and Preparation Procedures
Image Analysis Algorithms:
  Particle-Based Grey Level Segmentation
  Particle-Based Morphological Segmentation
  Particle-Based EDS Data Corroboration
Conclusion

## Slide 3: Introduction
Want to analyze mass percentages and particle size distributions (milling characteristics) of the phases that make up commercial cement, which heavily influence its physicochemical characteristics

## Slide 4: Potential Applications
Basis for additional research that depends on mass percentages or particle size distributions (i.e. hydration product, clinker size research):
Investigate competing cement formulas
Improve quality control for cement manufacturing processes such as milling

## Slide 5
BEI
EDS
SEM
Class | Average Grey Level | Circularity | Chemical Composition |  |  | 
 |  |  | Si | Al | Ca | Fe
A | … | … | … | … | … | …
B | … | … | … | … | … | …
C | … | … | … | … | … | …
… | … | … | … | … | … | …
EDS Segmentation
Simple Grey Level Segmentation

## Slide 6: Simple Grey Level Segmentation Problems
Cross-section polishing artefacts
Electro-magnetic distortion

## Slide 7: EDS Segmentation Problems
Large range of chemical compositions in phases such as fly ash
  Many kinds of crystal minerals,
  each with their own chemical
  composition
  Difficult to segment phases if fly ash has similar chemical composition to slag or clinker
Cannot accurately measure particles smaller than 1 micrometer

## Slide 8: Purpose of Investigation
Simple Grey Level Segmentation and EDS Segmentation are not accurate enough, can only implement simple segmentation classes based on pre-calculated information
Create new image analysis algorithms to segment the phases using more complex information and methods:
Particle-Based Grey Level Method
Particle-Based Morphological Method
Particle-Based EDS Data Corroboration
(New capability)

## Slide 9: Sample Information and Preparation Procedures
Particle-Based Grey Level Segmentation:
Clinker (57% mass) + Gypsum (3) + 4500 cm2/g Blaine Slag (40)
Particle-Based Morphology Segmentation:
Clinker (70) + Japanese Fly Ash (30)
Preparation Procedures:
Immersed in resin medium
Polished using cross-section polishing machine
Carbon covered for SEM-EDS measurements
At least 10 BEI images taken at 500X magnification for image analysis

## Slide 10: I. Particle-Based Grey Level Segmentation

## Slide 11: Particle-Based Grey Level Segmentation Principle
Images should be segmented by grey level in terms of particles, not pixels

## Slide 12
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Back-scattered Electron Image of Clinker and Slag 4500 Sample with Enlarged Particle

## Slide 13
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Grey Level Value
Number of Pixels
Histogram of Sample Image with Phase Grey Level Thresholds

## Slide 14
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Grey Level Segmented Sample Image with Enlarged Particle
Clinker | 
Slag | 
Gypsum | 
Fuzzy Area | 
Resin | 

## Slide 15
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Grey Level Value
Number of Pixels
Histogram of Sample Image with the Particle Grey Level Threshold

## Slide 16
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Particle Segmented Sample Image with Enlarged Particle

## Slide 17
Phase | Area Percentage
Slag | 92.34%
Clinker | 3.83%
Gypsum | 3.83%
Particle is classified as the phase with the highest area percentage.
So this particle is categorized as slag.
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Clinker | 
Slag | 
Gypsum | 
Fuzzy Area | 
Resin | 

## Slide 18
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Sample Image with Enlarged Particle (slag outlined in red)

## Slide 19
Raw Image
Particle Extraction
Pixel Classification
Particle Classification
Phase Images
Slag Only Sample Image with Enlarged Particle

## Slide 20
Chart: Clinker + Slag 4500 Phase Mass Percentages
| Mixed Value | Simple Grey Level Segmentation | Particle-Based Grey Level Segmentation
Clinker | 57 | 51.94 | 57.7
Slag | 40 | 37.6 | 40.56
Gypsum | 3 | 10.56 | 1.74

## Slide 21
Chart: Slag 4500 Size Distributions
Chart: Clinker Size Distributions

## Slide 22: II. Particle-Based Morphological Segmentation

## Slide 23: Particle-Based Morphological Segmentation Principle
Particles can separated in terms of morphology, not just grey level

## Slide 24
Particle Circularity Filtering
Hole Circularity Filtering
Raw Image
Phase Images
Particle Extraction
Back-scattered Electron Image of Clinker and Fly Ash Sample

## Slide 25
Particle Circularity Filtering
Hole Circularity Filtering
Raw Image
Phase Images
Particle Extraction
Particle
Resin
Histogram of Sample Image with the Particle Grey Level Threshold
Grey Level Value
Number of Pixels

## Slide 26
Particle Circularity Filtering
Hole Circularity Filtering
Raw Image
Phase Images
Particle Extraction
Particle Segmented Sample Image

## Slide 27
Circularity = 0.631
Circularity = 0.951
Phase | Average Circularity
Clinker | 0.633
Fly Ash | 0.947
Particle Circularity Filtering
Hole Circularity Filtering
Raw Image
Phase Images
Particle Extraction

## Slide 28
Particle Circularity Filtering
Hole Circularity Filtering
Raw Image
Phase Images
Particle Extraction
Circularity Filtered Sample Image

## Slide 29
Circularity = 0.433
Circularity = 0.960
Particle Circularity Filtering
Hole Circularity Filtering
Raw Image
Phase Images
Particle Extraction
Hole Circularity Filtered Sample Image with Enlarged Particle Image

## Slide 30
Particle Circularity Filtering
Hole Circularity Filtering
Raw Image
Phase Images
Particle Extraction
Fly Ash Phase Image

## Slide 31
Accurate results for clinker + Japanese fly ash sample
Other samples have yet to be investigated
Chart: Clinker + Japanese Fly Ash Phase Mass Percentages
| Mixed Value | Particle-Based Morphological Segmentation
Clinker | 70 | 70.37
Japanese Fly Ash | 30 | 29.63

## Slide 32: III. Particle-Based EDS Data Corroboration
(Part I + Part II + EDS)

## Slide 33: New Capabilities
Can compare both image analysis and EDS data (i.e. average grey level and chemical composition) in a single algorithm, which enables us to achieve more accurate results
EDS
Image Analysis
+

## Slide 34
Chart: Average Grey Level Vs. Clinker Area Percentage of Clinker + Slag 4500 Particles

## Slide 35: Conclusion
Can now measure complex features of particles such as hole circularity or particle area percentages
Particle-based grey level and morphological segmentation show great improvements in accuracy when measuring phase mass percentages and particle size distributions
Accuracy and efficiency can be improved by combining both image analysis and EDS data

## Slide 36: Image Analysis Issues
Accurate particle extraction
Minimum particle sample size for accurate results
Optimal image magnification

## Slide 39
FIN

## Slide 40: Area Categorization
1. Number of categories/phases
(clinker, slag, gypsum, fuzzy area, resin = 5)
2. Grey level threshold values
Notes: 40

## Slide 41: Grey Level Threshold Determination
Two Guidelines
Enclose Visible Histogram Features
Notes: 41

## Slide 42: Grey Level Threshold Determination
2. Maintain Particle Integrity
Notes: 42

## Slide 43: Naïve Grey Level Segmentation
Clinker + Slag System SEM-BSE Image
Image Grey Level Histogram
Notes: 43

## Slide 44: Naïve Grey Level Segmentation
Slag Areas Outlined in Red
Notes: 44

## Slide 45: Naïve Grey Level Segmentation
Slag Area Identification Issues
Notes: 45

## Slide 46: Streaking
Grey Level Range
190 – 230
Clinker Particle
Notes: 46

## Slide 47: Streaking
Clinker
Slag
Grey Level Range
190 – 230
Clinker Particle
Notes: 47

## Slide 48: Streaking
Arises from cross-section polishing imperfections
Many attempts with different settings, no success
Notes: 48

## Slide 49: Naïve Grey Level Segmentation
Slag Area Identification Issues
Notes: 49

## Slide 50: False Particles
Notes: 50

## Slide 51: False Particles
Notes: 51

## Slide 52: False Particles
Small effect on phase area percentage
Huge effect on particle size distribution
  Large particles get split
  Many small particles are created
Notes: 52

## Slide 53: Naïve Grey Level Segmentation
Slag Area Identification Issues
Notes: 53

## Slide 54: Edge Inclusion
 | Edge Removed | Edge Included
Average Grey Level | 209 | 199
Clinker-Slag Boundary = 200
Removing the edges makes classification easier and more accurate
Notes: 54